SPECIFICATION 901

CONCRETE – GENERAL WORKS

Copyright MAIN ROADS Western Australia

| REVISION REGISTER |  |  |  |
| --- | --- | --- | --- |
| Clause Number | Description of Revision | Authorised By | Issue Date |
| 901.01 | Clause amended to remove the term “non-structural” from general works | SDSE | 14/11/2025 |
| 901.04(2) | Fly ash has been added as part of blended cement | SDSE | 31/07/2025 |
| 901.02 | Roads to Reuse (RtR) Product Specification added | SDSE | 27/06/2023 |
| 901.06 | “CRC” and “RRC” definition added |  |  |
| 901.03 | Sustainability consideration clause added |  |  |
| 901.08 | Aggregate with sustainability consideration clause added |  |  |
| 901.09.02 | Maximum slump limit increased and shrinkage requirement added |  |  |
| 901.09.03 | Strength grade limit modified for normal class concrete |  |  |
| 901.02 | Added Australian Standard. Amended text for other Standards. | SBDE | 15/06/2018 |
| 901.03 | Added “and” against Constituents Deleted Para 4 - Aggregate Durability. |  |  |
| 901.04 | Amended text in paras 1, 2 and 4. Added new para 7 – Aggregate Durability |  |  |
| 901.06 | Clause “Admixtures” Added text para 2. |  |  |
| 901.07 | Deleted Clause “Reinforcement” |  |  |
| 901.09 | Deleted Clause “Formwork” |  |  |
| 901.30 | Clause “Curing and Protection”. Amended text para 1 |  |  |
| 901.32 | Clause “Concrete Surfaces” Deleted para 3. |  |  |
| 901.02 | Replaced reference “Water Services Specification Section SP43 – Cementitious Materials for Concrete” to ‘Australian Technical Infrastructure Committee (ATIC) Specification SP43 – Cementitious Materials for Concrete”. | SBDE | 21/07/2011 |
| 901.05 | Replaced all references WSS -SP43 to ATIC Specification SP43 |  |  |
| 901.02 | Added reference to WSS SP43 | SDE | 25/05/2009 |
| 901.05 | Added Clauses on Cement |  |  |
| Annexure 901A | Added Concrete Request for Registration form |  |  |
| 901.04 | New Clause added – titled ‘Aggregate’ | SDE | 26/06/2008 |
| Guidance Notes | Guidance Note concerning paving joints and surface finish added | SDE | 02/11/2006 |
| Whole document | Complete revision of Issue 5.0 to new format | MCP | 01/08/2006 |

CONTENTS

Clause	Page No

GENERAL	4

901.01	Scope	4

901.02	References	4

901.03	Definitions	5

PRODUCTS AND MATERIALS	6

901.04	Cement	6

901.05	Aggregate	6

901.06	Aggregate with Sustainability Consideration	7

901.07	Admixtures	8

901.08	Sustainability Considerations	8

901.09	Class of Concrete	8

901.10 – 901.25	NOT USED	9

OPERATIONS	9

901.26	General	9

901.27	Mixing of Concrete	9

901.28	Placing of Concrete	9

901.29	Testing	10

901.30	Curing and Protection	10

901.31	Concreting in Hot Weather	11

901.32	Concrete Surfaces	11

901.33	Conformance and Non-conformance	12

901.34 – 901.80	NOT USED	12

AS BUILT AND HANDOVER REQUIREMENTS	12

901.81 – 901.90	NOT USED	12

CONTRACT SPECIFIC REQUIREMENTS	12

901.91 – 901.99	NOT USED	12

ANNEXURE 901A	13

ATIC – Cementitious Materials for Concrete – Request for Registration by Manufacturer	13

SPECIFICATION 901

CONCRETE – GENERAL WORKS

| GENERAL |  |
| --- | --- |
| 901.01 Scope |  |
| The work under this specification consists of the mix design, the supply and delivery, placing, compaction, finishing, curing and protection of concrete for general works where normal (N) class concrete has been specified. |  |
| Concrete for bridgeworks, manufacture of reinforced concrete box culverts and other major structures is covered in Specification 820 CONCRETE FOR STRUCTURES. | Major Concrete Structures |
| 901.02 References |  |
| - Australian Standards, Main Roads Western Australia Test Methods, Main Roads Western Australia Standards and Main Roads Western Australia Specifications are referred to in abbreviated form (e.g. AS 1234, MRS 67-08-43 or WA 123). For convenience, the full titles are given below: |  |
| Australian Standards |  |
| AS 1012 Methods of Testing Concrete |  |
| AS 1379 Specification and Supply of Concrete |  |
| AS 1478.1 Chemical Admixtures for Concrete, mortar and grout – Admixtures for concrete AS 1478.2 Chemical Admixtures for concrete, mortar and grout – Methods of sampling and testing admixture for concrete, mortar and grout |  |
| AS 27581 Aggregates and Rock for Engineering Purposes Part 1: Concrete Aggregates |  |
| AS 3600 Concrete Structures. |  |
| AS 3610.1 Formwork for Concrete – Part 1: Documentation and surface finish |  |
| AS 3799 Liquid Membrane-forming Curing Compounds for Concrete |  |
| AS 3972 General Purpose and Blended Cements |  |
| Australian/New Zealand Standards |  |
| AS/NZS 4671 Steel Reinforcing Materials |  |
| Other Standards |  |
| Australian Technical Infrastructure Committee (ATIC) Specification SP43 – Cementitious Materials for Concrete |  |
| Waste Authority WA Roads to Reuse (RtR) Product Specification – recycled road base and recycled drainage rock |  |
| Main Roads Specifications |  |
| Specification 201 QUALITY MANAGEMENT |  |
| Specification 819 FALSEWORK |  |
| Specification 820 CONCRETE FOR STRUCTURES |  |
| Specification 821 FORMWORK |  |
| Specification 822 STEEL REINFORCEMENT |  |
| 901.03 Definitions |  |
| 901.03.01 GENERAL |  |
| - Concrete in general shall consist of a mixture of cement, water, coarse aggregate and fine aggregate. | Constituents |
| The strength of concrete shall be defined as the average 28 day compressive strength of a minimum of two standard 100mm diameter by 200 mm long cylinders taken from the same sample and made and cured and tested in accordance with AS 1012. | Strength |
| Crushed Recycled Concrete (CRC), as used in the waste recycling industry in Western Australia, refers to processed (crushed and blended) materials recovered from construction and demolition waste, predominantly comprising concrete with other secondary materials managed under the Roads to Reuse (RtR) Specification. | CRC |
| Recycled Returned Concrete (RRC) refers to processed (crushed and blended) materials recovered from returned hardened concrete (with no other secondary materials). | RRC |
| 901.03.02 FINISHED CONCRETE |  |
| - In its finished state the concrete shall be sound, dense, durable, free from honeycombing and shall have the strength and other properties specified. | Finished State |
| The exposed surfaces shall be smooth and dust free and conform to the shape tolerances specified. |  |
| Concrete shall comply with AS 1379 except as varied by the requirements of this Specification. |  |
| PRODUCTS AND MATERIALS |  |
| 901.04 Cement |  |
| - Unless otherwise specified, all cement used in the works shall comply with the requirements of Type GP cement as specified in AS 3972 and Australian Technical Infrastructure Committee (ATIC) Specification SP43. The Contractor shall provide manufacturer’s test certificates showing all cement has been sampled, tested and conforms in all respects with AS 3972 and ATIC Specification – SP43. | Testing |
| Blended cement shall be a combination of Type GP cement and ground granulated iron blast-furnace slag complying with AS 3582.2 and ATIC – Specification SP43 or fly ash complying with AS/NZS 3582.1 and ATIC – Specification SP43. The silica fume to be added to the blended cement shall be finely divided and comply with AS/NZS 3582.3 and ATIC – Specification SP43. | Blended Cement |
| Cement for manufacture of concrete shall comply with the requirements of ATIC – Specification SP43. The Cementitious Material Registration Scheme (CMRS) shall be used to confirm that the cement complies with ATIC – Specification SP43. The standard application form for CMRS registration is given in Annexure 910A. | Certification |
| Prior to manufacturing of concrete the Contractor shall confirm that the cement complies with ATIC – Specification SP43 and shall provide the CMRS registration number for the cement to the Superintendent for approval of the cement. | HOLD POINT |
| The Contractor shall use cement in approximately the chronological order in which it is delivered from the manufacturer. Transportation units and storage bins for bulk cement shall be weatherproof and shall be constructed so that there is no dead storage. The Contractor shall demonstrate that the storage bins for bulk cement do not have any dead storage. If dead storage exists the bins shall be emptied completely at least once every three months. Cement delivered in bags shall be stored in weatherproof structures having floors raised above the ground. Cement that is more than three months old shall not be used. |  |
| Concrete manufactured from cement not conforming to this Specification or from cement that has deteriorated and become unsuitable for use shall be rejected |  |
| 901.05 Aggregate |  |
| - Fine aggregates for concrete shall be natural sand or a combination of natural and manufactured sand and shall comply with the requirements of AS 2758.1. The maximum amount of water absorption for fine aggregates shall not exceed 1.5 percent and 2.5 percent respectively. | Fine Aggregates |
| Coarse aggregates for concrete shall be crushed igneous rock or crushed or screened river gravel or crushed concrete returns conforming to the requirements of AS 2758.1. The maximum amount of water absorption for coarse aggregates shall not exceed 2.5 percent. | Coarse Aggregates |
| The durability of coarse aggregates shall be assessed according to test methods of AS 2758.1. The acceptance criteria for these tests shall be that for a concrete exposure classification C unless otherwise specified. | Durability |
| All aggregate proposed for use in the Works shall comply with the requirements of the "Alkali-Reactive Materials" clause of AS 2758.1. Aggregates that are classified as slowly-reactive or reactive shall not be used. | Alkali-Reactive Materials |
| The Contractor shall provide proper means of storing the aggregates. Each nominal size of coarse aggregate and fine aggregate shall be kept separated and suitable precautions shall be taken to prevent the aggregates from being contaminated by the ground or by wind-blown dust or other foreign matter. | Storage |
| The grading of the individual aggregates shall conform to the limits for these materials given in AS 2758.1. Sampling for the purposes of carrying out tests shall be in accordance with AS 1141. | Testing |
| Aggregates shall meet the durability criteria for concrete exposure classification C of AS 2758.1. | Aggregate Durability |
| 901.06 Aggregate with Sustainability Consideration |  |
| - Fine aggregates for concrete shall be natural sand or a combination of natural and manufactured sand and shall comply with the requirements of AS 2758.1. | Fine Aggregates |
| Coarse aggregates for concrete shall be crushed igneous rock or crushed or screened river gravel or crushed concrete returns conforming to the requirements of AS 2758.1. | Coarse Aggregates |
| The durability of the blended coarse aggregates shall be assessed according to test methods of AS 2758.1. The acceptance criteria for these tests shall be that for a concrete exposure classification B2 of AS 2758.1 unless otherwise specified. | Durability |
| All aggregate source proposed for use in the Works shall comply with the requirements of the “Alkali-Reactive Materials: clause of AS 2758.1. Aggregates that are classified as slowly-reactive or reactive shall not be used. | Alkali-Reactive Materials |
| The Contractor shall provide proper means of storing the aggregates. Each nominal size of coarse aggregate and fine aggregate shall be kept separated and suitable precautions shall be taken to prevent the aggregates from being contaminated by the ground or by wind-blown dust or other foreign matter. | Storage |
| The grading of the individual aggregates shall conform to the limits for these materials given in AS 2758.1. Sampling for the purposes of carrying out tests shall be in accordance with AS 1141. | Testing |
| Aggregates shall meet the durability criteria for concrete exposure classification B2 of AS 2758.1. | Aggregate Durability |
| 901.07 Admixtures |  |
| - Admixtures may be used in concrete to modify workability but will not be permitted for the purpose of reducing cement content. However, the admixture shall have no harmful effect whatsoever upon the quality of the concrete or upon any reinforcement or other fixture embedded therein. | Admixtures Compliance |
| Any admixture when tested in accordance with AS 1478.2, shall comply with the requirements of and be used in accordance with AS 1478.1. |  |
| 901.08 Sustainability Considerations |  |
| - Materials for used for concrete for general works shall be managed under the sustainability hierarchy of REDUCE, REUSE and RECYCLE. |  |
| Unless defined otherwise, the materials described in this specification shall be sourced from pits or quarries of natural materials, and shall be blended, crushed or processed as applicable to produce a homogenous material. These materials are a finite resource and waste shall be reduced to a minimum. |  |
| The term REUSE refers to the reuse (or rehabilitation or rejuvenation) of end-of-life (or defective or waste) materials in products for the same purpose. Where practical, redundant concrete materials and plant waste should be recovered and reused, or otherwise recycled to the highest level use practical. |  |
| The term RECYCLE refers to the reprocessing of end-of-life (or defective or waste) materials into new repurposed products. This specification also includes manufactured materials sourced from recycled Construction and Demolition Waste such as Crushed Recycled Concrete (CRC) or Recycled Returned Concrete (RRC). Recycled materials for general concrete shall be blended, crushed or processed as applicable to produce a homogenous material by a recycling premises. Recycled materials shall only be included in materials which are designated as recycled |  |
| 901.09 Class of Concrete |  |
| - The Class of concrete shall be Normal-class as specified on the Drawings. | Normal Class Concrete |
| Unless otherwise noted slump and aggregate size is as follows: |  |
| - Maximum aggregate size 20 mm | Aggregate Size |
| - Maximum slump 120 mm | Slump |
| - Maximum 56 days drying shrinkage as per AS 1379 | Shrinkage |
| Specifying Supply Parameters for Normal-class Concrete. Normal-class concrete shall be specified in accordance with AS 1379 including all of the following: | Concrete Supply |
| - Standard strength grade to be designated as one of N20, N25, N32 or N40. CRC or RRC can only be used in concrete grade up to N32; | Strength Grade |
| - The slump at point of acceptance; |  |
| - Intended method of placement; |  |
| - The maximum nominal size of aggregate; and |  |
| - Project assessment to provide additional test data if required by the supplier. |  |
| 901.10 – 901.25 NOT USED |  |
| OPERATIONS |  |
| 901.26 General |  |
| - Requirements for falsework shall be in accordance with Specification 819 FALSEWORK. | Falsework |
| Requirements for formwork shall be in accordance with Specification 821 FORMWORK. | Formwork |
| Requirements for steel reinforcement shall be in accordance with Specification 822 STEEL REINFORCEMENT. | Reinforcement |
| 901.27 Mixing of Concrete |  |
| - Production and delivery for the concrete shall be in accordance with the requirements of AS 1379 except that additional water shall not be introduced into a mixed batch of concrete and the period for completion of discharge from the commencement of mixing shall not exceed 90 minutes. | Batch Plant and Transit Mixers |
| 901.28 Placing of Concrete |  |
| - Prior to the placement of any concrete, the Contractor must certify to the Superintendent that all falsework, formwork, reinforcement, levels, placement procedures and curing procedures to be employed comply with the requirements of the Technical Specification. | HOLD POINT |
| Before commencement of each concrete pour the Contractor must demonstrate to the Superintendent that sufficient vibrators and spares are available and tested. The number of working vibrators required must not be less than one for each 4 cubic metres of concrete placed per hour. The number of standby vibrators must not be less than 25% of the number of working vibrators with a minimum of one. | HOLD POINT |
| Concrete shall be conveyed from onsite mixers to its final position without delay and by methods which will not permit segregation and/or loss of material. All the concrete shall be placed in its final position within 90 minutes of the materials having been placed in the mixer. | Transport and Placing |
| Concrete shall be placed in a manner which will prevent segregation. Concrete shall be spread in horizontal layers with the first layer not exceeding 350mm in compacted thickness and the thickness of subsequent layers limited to 75% of the length of the immersion vibrators used. Placing shall be continuous between specified or approved construction joints. |  |
| During placing, concrete shall be compacted using mechanical or pneumatic immersion vibrators to remove all voids and air bubbles. Immersion vibrators shall have a frequency of not less than 150 Hertz and, where concrete Class 2 or 3 finish is specified, shall be fitted with approved rubber caps. The largest practical size of vibrator should be used. | Vibration |
| Care shall be taken during placing to see that no foreign substances are included in the concrete. | Foreign Substances |
| The location of all construction joints shall be as indicated on the Drawings or approved by the Superintendent. Construction joints shall be made on true vertical and horizontal planes and the surface shall be roughened to remove all laitance and expose the aggregate to provide a thorough bond with concrete cast subsequently. The roughened surface shall be thoroughly cleaned with water to remove loose chips and any foreign matter. Immediately before fresh concrete is cast against the joint the hardened concrete surface shall be thoroughly wetted. | Construction Joints |
| 901.29 Testing |  |
| 901.29.01 GENERAL |  |
| - All minor structural works shall be tested in accordance with sub clauses 2 and 3 below and in accordance with Structural Concrete quality verification requirements in Specification 201 QUALITY MANAGEMENT. General non-structural concrete works may be accepted on the basis of project testing certification, provided by the concrete supplier. | Testing Requirements |
| Sampling and testing of concrete specimens shall be in accordance with AS 1012 Parts 1 to 18. Concrete test cylinders shall be 100mm diameter by 200mm long. Rubber caps may be used for the capping of test cylinders, as allowed in AS 1012.9. | Sampling Testing |
| The Contractor shall have available not less than 6 concrete moulds, slump cone and tray, and rod. |  |
| 901.29.02 COMPRESSIVE STRENGTH ANALYSIS |  |
| - Any batch of concrete shall be deemed to comply with the strength requirements of this specification if: - Every concrete test specimen in the batch has a 28 day compressive strength greater than 90% of the characteristic strength; and - The average 28 day compressive strength of the concrete test specimens in the batch is equal to or greater than the characteristic strength in accordance with AS1379. | Compliance |
| 901.30 Curing and Protection |  |
| - Freshly placed concrete shall be protected from the sun, wind and rain and prevented from drying out too quickly. |  |
| All concrete surfaces shall be cured by one of the following methods for not less than five (5) days: - Continuous wetting. - Spraying with an approved curing compound complying with the requirements of AS 3799. Such curing compound shall be applied in accordance with the manufacturer's published recommendations. - Wrapping with polythene or similar film to provide an airtight cover. - Maintaining the formwork in position for the curing period. |  |
| The Contractor shall ensure that the method of curing shall not result in any staining of exposed surfaces of concrete. |  |
| 901.31 Concreting in Hot Weather |  |
| - The requirements of AS 1379 for temperature of the concrete at the point of discharge shall be met for all concrete works undertaken in hot weather. In addition, placement of concrete shall only be permitted providing: | Placement Temperature |
| - the concrete mix temperature during placement shall at no time exceed 35°C, - AND, EITHER | Mix Temperature |
| - the ambient shade temperature does not exceed 38°C and is falling, - OR | Shade Temperature |
| - the ambient shade temperature is less than 38°C and rising provided that the placement can be completed before the ambient temperature exceeds 38°C. |  |
| 901.32 Concrete Surfaces |  |
| - The type of formed concrete surface finish shall be as shown on the Drawings and shall comply with the requirements of Section 3 of AS 3610.1. | Formed Surface Finish |
| The type of unformed surface finish shall be as shown on the Drawings and shall be in accordance with Table 901.1 below. | Unformed Surface Finish |

TABLE 901.1	UNFORMED SURFACE FINISHES FOR CONCRETE

| Designated Finish | Type of Concrete Finish | Maximum Allowable Surface Irregularities |
| --- | --- | --- |
| U1 | A wood floated finish to produce a uniform surface without surface pitting or cavities | 5 mm abrupt or 15 mm in a 3 m template |
| U2 | A high quality steel trowelled finish having a dense smooth impervious finish without surface pitting or cavities | Nil abrupt or 5 mm in a 3 m template |
| U3 | A high quality mechanical steel trowelled finish having a dense impervious finish without surface pitting or cavities | 2 mm abrupt or 5 mm in a 3 m template |
| U4 | A wood floated surface with a broomed finish | 2 mm abrupt or 5 mm in a 3 m template |

| 901.33 Conformance and Non-conformance |  |
| --- | --- |
| - Concrete that shows evidence of poor workmanship such as honeycombing or is porous due to inadequate compaction or due to segregation or concrete that fails to comply with this Specification in regard to strength or tolerances or finishes or other requirements shall be deemed to be non-conforming. | Non-conforming |
| If at any time the concrete fails to meet any of the requirements of this specification, concreting operations shall be suspended until corrective measures are taken, at no cost to the Principal. | Operations Suspended |
| 901.34 – 901.80 NOT USED |  |
| AS BUILT AND HANDOVER REQUIREMENTS |  |
| 901.81 – 901.90 NOT USED |  |
| CONTRACT SPECIFIC REQUIREMENTS |  |
| 901.91 – 901.99 NOT USED |  |

ANNEXURE 901A

ATIC – Cementitious Materials for Concrete – Request for Registration by Manufacturer

| Cement or Blend Details |  |
| --- | --- |
| Product Name |  |
| Type |  |
| Proportions |  |
| Manufacturer |  |
| Place of Manufacture |  |
| Source of Constituent Materials |  |
| Cement Clinker |  |
| Fly Ash |  |
| Slag |  |
| Limestone |  |
| Gypsum |  |
| Grinding Aids |  |
| Supply Details |  |
| Dispatching Supplier |  |
| Contact Name |  |
| Contact Phone No. |  |
| Contact Address |  |
| Suppliers ABN |  |

Send this form with the sample to:

RTA Chemical and Materials Laboratory

Att: Laboratory Officer

Unit H, 75 St. Hilliers Rd,

Auburn NSW 2144

For RTA Laboratory Use Only:

Date of Registration:

Registration No:

GUIDANCE NOTES

FOR REFERENCE ONLY – DELETE GUIDANCE NOTES FROM FINAL DOCUMENT

- All edits to this specification are to be made using track changes, to clearly show added/ deleted text.

If all information relating to a clause is deleted, the clause number should be retained and the words “NOT USED” should be inserted.

The proposed document with tracked changes must be submitted to the Project Manager for review, prior to finalising the document.

Once the Project Manager’s review is complete, accept all changes in the document, turn off track changes and refresh the Table of Contents.

The Custodian of this specification is Senior Bridge Design Engineer.

CLAUSE 901.09	CLASS OF CONCRETE

The project manager shall select the appropriate concrete Grade in Clause 901.09.3

CONCRETE PAVING

The project manager shall ensure that construction/contraction/expansion joint details and the paving surface finish are preferably included on the Contract Drawings or failing this that details are clearly described within the Contract Specific Requirements section of the Specification.

CONTRACT SPECIFIC REQUIREMENTS

The following clauses are to be placed under the CONTRACT SPECIFIC REQUIREMENTS, as required.  After inserting the clause, change the clause number and heading to style “H2 SP” so it appears in the Table of Contents.

| XXX.XX SUB-HEADING (H2 SP) |  |
| --- | --- |
| - Insert text (Main Table SP) | XXXX |
| Insert text (Main Table SP) |  |
| XXX.XX SUB-HEADING (H2 SP) |  |
| - Insert text (Main Table SP) |  |
| Insert text (Main Table SP) |  |

AMENDMENT CHECKLIST

| Specification No. | 901 | Title: | CONCRETE – GENERAL WORKS |  |  |  | Revision No: |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Project Manager: |  |  |  |  | Signature: |  |  | Date: |  |
| Checked by: |  |  |  |  | Signature: |  |  | Date: |  |
| Contract No: |  |  |  | Contract Name: |  |  |  |  |  |

| ITEM | DESCRIPTION | SIGN OFF |
| --- | --- | --- |
| Note: All changes/amendments must be shown in tracked changes until approved. |  |  |
|  | Project Manager has reviewed the specification and identified additions and amendments. |  |
|  | Standard clauses amended? MUST SEEK approval from the Specification Custodian. |  |
|  | Any unlisted materials/products proposed and approved by the Project Manager? If “Yes” provide details at 16. |  |
|  | Deleted clauses shown as “NOT USED”. |  |
|  | Ensure appropriate INSPECTION AND TESTING parameters are included in Specification 201 (test methods, minimum testing frequencies verified). |  |
|  | AS-BUILT AND HANDOVER requirements addressed. |  |
|  | CONTRACT SPECIFIC REQUIREMENTS addressed? Contract specific materials, products, clauses added? (refer Specification Guidance Notes). |  |
|  | ANNEXURES completed (refer Specification Guidance Notes). |  |
|  | Estimates Manager has approved changes to SMM. |  |
|  | Project Manager certifies completed specification reflects intent of the design. |  |
|  | Independent verification of completed specification arranged by Project Manager. |  |
|  | Project Manager’s review completed. |  |
|  | SPECIFICATION GUIDANCE NOTES deleted. |  |
|  | TABLE OF CONTENTS updated. |  |
|  | FOOTER updated with Document No., Contract No. and Contract Name. |  |
|  | Supporting information prepared and submitted to Project Manager. |  |
| Additional information or further action: |  |  |

| Signed: | (Project Manager) | Date: |  |
| --- | --- | --- | --- |